## Slide 1: PowerPoint 8: Processing techniques
PowerPoint presentation
6. Materials and their properties
6.3 The effects of processing techniques on materials

## Slide 2: Objectives
PowerPoint presentation
By the end of this session, learners should be able to:
understand how processing techniques affect material properties.

## Slide 3: Materials processing
When processing a material it is possible to alter its properties.
This is predominantly done by modifying:
grain structure
composition.

## Slide 4: Metal forming, reshaping and plastic deformation
In general, metal forming is a broad term that encompasses a number of manufacturing processes. However, the one characteristic that all metal forming processes share is the reshaping of raw metal stock into a finished part.
Reshaping is achieved through a mechanical process that is referred to in the material sciences as plastic deformation.
The plastic deformation of material occurs by applying force greater than the yield strength of the material. Once the force is applied, the change in physical shape of the material cannot be undone.

## Slide 5: Bending
Bending is a flexible metal forming process which utilises a brake press or similar type of press machine. The metal sheet is formed by placing it over a die block that punch-presses the material.
The die does not actually punch a hole in the metal sheet but creates a bending force that shapes the metal to the die.

## Slide 6: Rolling
Rolling in metalworking is a metal forming process that helps to reduce the thickness of metal and make the thickness uniform. The metal stock is passed through one or more pairs of rolls to reduce the material.
Rolling is classified according to the temperature of the metal rolled. If the temperature of the metal is above its recrystallisation temperature it is known as hot rolling. If the temperature of the metal is below the recrystallisation temperature, it is known as cold rolling.

## Slide 7: Hot rolling
The hot rolling process has a significant effect on the properties of steel, by heating steel above its recrystallisation temperature and then cooling it at room temperature in a process known as normalisation.
The steel’s microstructure undergoes permanent changes, resulting in enhanced toughness and ductility. This additional ductility makes the metal easy to form and bend. The hot rolling process also affects the overall shape of the finished metal piece. Hot rolled forms can be much larger than cold rolled forms. However, since hot rolled steel is heated and cooled, it is susceptible to shrinkage, giving less control over the shape and size of the finished product.

## Slide 8: Hot rolled steel process

## Slide 9: Roll forming
Similar to rolling, roll forming is a process that shapes metal as it passes through successive sets of rollers in a machine. As the metal is conveyed through the machine, pairs of rollers continuously form and bend the sheets or strips into the desired cross-sectional shape.
The process is performed incrementally, gradually forming the part until the desired cross section is achieved. Roll forming is generally used to produce components with long lengths or for large production runs.

## Slide 10: Hot vs cold working
As with rolling, the key difference between hot working and cold working is that hot working is performed at temperatures above the recrystallisation temperature of the metal whereas cold working is done at temperatures below the recrystallisation temperature of the metal.

## Slide 11: Hot working
The recrystallisation temperature is the temperature at which the deformed grains are replaced by defect-free grains in the metal. This allows the metal to recrystallise while plastically deforming. This process occurs below the melting point of the metal.
The deformation and the recovery of the metal take place simultaneously. The temperature limits of the hot working process are determined by the characteristics of the metal, as as noted, hot working is performed at temperatures above the recrystallisation temperature.
During the hot working process, internal or residual stresses are not built in. Hot working can be used to produce a finished product as it can remove cracks and faults. The hot working process is important in increasing the ductility of metal. The yield strength can be reduced using this process.

## Slide 12: Cold working
Cold working or work hardening is the process of strengthening a metal by plastic deformation at temperatures below the recrystallisation temperature.
Strengthening is achieved by dislocation movements of the metal structure and without heat. A dislocation is defined as a crystallographic defect in the metal crystal system.
During cold processing, no significant recovery takes place. Internal and residual stresses build up in the metal. Cracks or pores may propagate, and new cracks may form during the process.

## Slide 13: Hot and cold working table
 | Hot working | Cold working
Temperature | Hot working is performed at temperatures above the recrystallisation temperature of the metal | Cold working is performed at temperatures below the recrystallisation temperature of the metal
Stress | In hot working, no internal and residual stresses build up in the metal | In cold working, internal and residual stresses build up in the metal
Recovery | Deformation of the metal and its recovery occurs simultaneously | No significant metal recovery takes place
Cracks | Cracks are pores can be removed | Cracks propagate, and new cracks are formed
Uniformity | The uniformity of the metal is very high | The uniformity of the metal is low

## Slide 14: Stretching
Another form of metal processing, this forming process stretches and bends the workpiece simultaneously over a die to form complex or large contoured parts.
In stretching, the deformation of the sheet occurs through radial strain. The process is used to shape large parts that require sizeable, accurate radius bends with smooth surfaces.

## Slide 15: Deep drawing
Deep drawing is a common metal forming process. It is a method in which the metal sheet is clamped in place over a cavity-shaped die to form hollow-shaped components.
The motion of the punch pushes down, drawing it into the cavity. The tensile strength applied to the metal sheet is deformed to the external shape of the part.

## Slide 16: Sintering
Sintering, which is also called ‘frittage’, is the process of forming a solid mass of material through heat and pressure without melting to the point of liquefaction.
The process involves the atoms in the material diffusing across the particle boundaries and fusing together into one piece. Sintering occurs naturally in mineral deposits, and is used as a manufacturing process for materials including ceramics, metals and plastics.

## Slide 17: Sintering
In sintering, the porous spaces between the material’s particles are minimised during the process as the material is squeezed together under high temperature and pressure. This increases some of the material’s properties, including:
thermal and electrical conductivity
material strength
translucency.

## Slide 18: Sintering
The purpose of sintering is to impart strength and integrity to the material.
During the sintering process the temperature must be kept below the melting point of the constituent materials.
The picture shows the powdered metal which is compacted and sintered in this process.

## Slide 19: Powder coating
There are two types of powder coating, thermosets and thermoplastics (see also Session 6).
Thermoplastic powder coating finishes become liquid and very soft when heated. This eliminates chemical bonding. This process makes the powder coating both reversible and reusable.
Thermoset powder forms chemical bonds once cured, making it impossible to recycle it. It is suitable for high heat areas because the bonds prevent it from melting.

## Slide 20: Casting
Casting of materials falls into three groups, distinguished by the nature of the mould design:
expendable mould
permanent mould
composite mould.

## Slide 21: Casting types
Metal casting
Permanent mould
Expendable mould
Composite mould
Die casting
Gravity casting
Centrifugal casting
Permanent pattern
Expendable pattern
Sand casting
Plaster moulding
Ceramic mould
Lost foam casting
Investment casting

## Slide 22: Sand casting
Sand casting is the most common type of expendable mould casting, which generally uses permanent patterns to create the mould.
Molten metal is poured into an expendable sand mould cavity by gravity or force, where it solidifies to form the cavity shape part.

## Slide 23: Plaster mould casting and shell moulding
In plaster mould casting, the mould is made of plaster of Paris instead of sand and the process works in a similar way to sand casting.
Shell moulding uses a thin shell mould, of approximately 9mm. The mould is sand-bound together using a thermosetting resin binder.

## Slide 24: Injection moulding
Plastic injection moulding is the process of melting plastic pellets (thermosetting/thermoplastic polymers). Once malleable enough, the pellets are injected at pressure into a mould cavity, which fills and solidifies to produce the final product.

## Slide 25: Injection moulding materials
Acrylic (PMMA)
Poly(methyl methacrylate) is better known as PMMA or acrylic. It is a strong, clear thermoplastic that provides a lighter weight, shatter-resistant alternative to glass. Because PMMA is transparent and has excellent optical clarity, it allows a high percentage of light to pass through it.
Acrylonitrile butadiene styrene (ABS)
ABS is an engineering-grade thermoplastic with a relatively low melting point that makes it easy to mould. This opaque polymer supports the use of colourants and is available with different textures and surface finishes. ABS is known for its strength and impact resistance. It is corrosion resistant and, as it is a non-metallic material, it also retains a level of flexibility to absorb impact and thermal shock.

## Slide 26: Injection moulding materials
Polycarbonate (PC)
PC plastics are strong, tough materials that are naturally transparent. Their properties are similar to PMMA, but polycarbonate maintains its physical properties over a wider temperature range. When pigmented, PC maintains its colour over time and retains its strength.
Polyethyelene (PE)
HDPE and LDPE both share useful properties such as chemical resistance, but they differ in terms of their respective hardness, flexibility, melting point and optical transparency.

## Slide 27
Any questions?
‘T-LEVELS’ is a registered trade mark of the Department for Education. ‘T Level’ is a registered trade mark of the Institute for Apprenticeships and Technical Education.